名称: 滚珠轴承式耐磨试验机

其他名称：混凝土耐磨试验机  混凝土滚珠轴承式耐磨试验机

型号NS-2

荣计达产品编号HT93   7666元

一、概述：适用于按国标GB/T16925-1997，混凝土及其制品耐磨性试验方法，对混凝土及其制品、路面砖、地面砖、人造大理石、水磨石等建筑材料进行耐磨试验。

1. Overview: Applicable to test methods for abrasion resistance of concrete and its products in accordance with the national standard GB/T16925-1997, to conduct abrasion resistance tests on concrete and its products, pavement tiles, floor tiles, artificial marble, terrazzo and other building materials。

二、技术参数：

★磨头：13*15.875mm滚珠轴承

★磨头上的压力负荷： 154±2.5N

★转轴负荷额定转速：1000-1050r/min

★磨石工作硬度：大于HRC62

★测量行程：10mm

★噪音 ：≯75dB

★适和试件规格受磨面积：≮100*100mm≯300*300mm

★电机功率 ：0.75kw

★外形尺寸（长*宽*高）：700*450*800mm

★净重：163kg

2. Technical parameters:

★Grinding head: 13*15.875mm ball bearing

★Pressure load on the grinding head: 154±2.5N

★Rated speed of shaft load: 1000-1050r/min

★Working hardness of grindstone: greater than HRC62

★Measuring stroke: 10mm

★Noise: ≯75dB

★Abrasion area of suitable test piece specification: ≮100*100mm≯300*300mm

★Motor power: 0.75kw

★Dimensions (length * width * height): 700*450*800mm

★Net weight: 163kg

三、安装与使用：

★本机采用木箱包装，开箱后应检查产品合格证，集装单，使用说明书等资料是否全，并根据产品装箱查对箱内物件是否完备相符。

★打开箱检验合格的试验机应水平放在工作台上，本机不需要特别基础和地脚螺栓，只要保证水平和稳定性****可以。

★插上进水管并与水源接通，插上出水管，本机的四芯插头接控接上三相380V交流电源，并可靠接地，即可投入使用。

★将试件的受磨面朝上，放入试件夹具架内，试件夹具架内有移动板，可根据试件不同宽度变进行调整，通过水平调盘，将受磨面调整水平位置后，转动压紧螺杆夹紧试件。

★将磨头放在受磨面上，转动升降手柄使机架和中空转轴下降并压在磨头上，磨头的滚珠应全部对准中空转轴下端滚道，谨防中空转轴碰磨头上传感器

★继续转动升降手柄，使机架继续下降至传感器的顶部与红刻线对齐，同时，百分表的测量杆应与顶板相接触，并应有5mm的里程。

★转紧锁紧手柄板上防护罩开启水源，待水中空转轴内不断流向试件的受磨面时，开始试验。

★按下控制器的“欲动”按钮，电机开始工作，当磨头转30转左右时，自动停止，记下百分表的读书，按下“复位”按钮，使数码显示复零。然后再按下“起动”按钮，本机即开始运转，当磨头转至1000转时，自动停止记下百分表的读数，再一次按下“起动”按钮，本机继续运转而后，每转1000转，磨头**会自动停止，同时记下百分表读数，但转满5000转时，本机自动停转并自锁。要使本机重新运转，必须按下“复位”按钮，方可使本机正常运转，本机运转过程中，如要暂停试验，可按下“停止”按钮，即停转数据自动保存，以便试验数据的连续性。完整性和准确性。

★本机机架不能旋转。

★试验结束，关闭水源和电源，取出试件。

3. Installation and use:

★This machine is packed in wooden boxes. After opening the box, check whether the product certificate, assembly list, instruction manual and other materials are complete, and check whether the contents of the box are complete and consistent according to the product packing.

★The testing machine that passes the box inspection should be placed horizontally on the workbench. The machine does not need special foundation and anchor bolts, as long as the level and stability are guaranteed.

★Plug in the water inlet pipe and connect to the water source, plug in the water outlet pipe, the four-core plug of this machine is connected to the three-phase 380V AC power supply, and is reliably grounded, then it can be put into use.

★Put the abraded surface of the test piece facing up and put it into the fixture frame of the test piece. There is a movable plate in the fixture frame of the test piece, which can be adjusted according to the different widths of the test piece. Adjust the horizontal position of the worn surface through the horizontal adjustment plate. Then, rotate the compression screw to clamp the test piece.

★Place the grinding head on the surface to be ground, turn the lifting handle to lower the frame and the hollow shaft and press it on the grinding head. All the balls of the grinding head should be aligned with the raceway at the lower end of the hollow shaft. Beware of the hollow shaft touching the sensor on the grinding head.

★Continue to turn the lifting handle to make the rack continue to descend until the top of the sensor is aligned with the red engraved line. At the same time, the measuring rod of the dial indicator should be in contact with the top plate and should have a mileage of 5mm.

★Turn and lock the protective cover on the handle plate to turn on the water source, and start the test when the water in the idling shaft continues to flow to the worn surface of the test piece.

★Press the "to move" button of the controller, the motor starts to work, when the grinding head rotates about 30 revolutions, it will automatically stop, write down the reading of the dial indicator, and press the "reset" button to reset the digital display to zero. Then press the "start" button again, the machine will start to run, when the grinding head rotates to 1000 revolutions, it will automatically stop recording the readings of the dial indicator, press the "start" button again, the machine will continue to run and every time When it rotates 1000 revolutions, the grinding head** will automatically stop, and the reading of the dial indicator will be recorded at the same time, but when the revolution reaches 5000 revolutions, the machine will automatically stop and self-lock. To restart the machine, you must press the "Reset" button to make the machine run normally. During the machine's operation, if you want to suspend the test, you can press the "Stop" button to automatically save the stop data so that Continuity of test data. Completeness and accuracy.

★The machine frame cannot be rotated.

★After the test is over, turn off the water source and power supply and take out the test piece.

结构：如图：

Fourth, structure: as shown in the figure:

主机由底座（1），立柱（13），机架（11），电机（15），中空转轴（5），磨头（滚珠轴承）（4），试件夹具（2）等组成。电机（15）与机架（11）连接，通过皮带（12）带动中空转轴（5）工作时，中空转轴在垂直方向无约束，中空转轴（5）和配垂（10）辅件的自重全部压在磨头上。

The host is composed of a base (1), a column (13), a frame (11), a motor (15), a hollow shaft (5), a grinding head (ball bearing) (4), a test fixture (2), etc. The motor (15) is connected with the frame (11), and when the hollow shaft (5) is driven by the belt (12) to work, the hollow shaft is unconstrained in the vertical direction, and the weight of the hollow shaft (5) and the accessories (10) are all Press on the grinding head.

五、维护和保养：

1、试验结束后，将试验机，主柱及所有工作部分把谁擦干，然后加上防锈油。

2、本机传动部分定期加润滑油，不使用时应每月运转一次。

3、使用过程中，应经常检测磨头滚珠直径，小于15.675MM必须更换。

5. Maintenance and maintenance:

1. After the test, wipe the test machine, main column and all working parts dry, and then add anti-rust oil.

2. Lubricate the transmission part of the machine regularly, and run it once a month when not in use.

3. During use, the diameter of the grinding head ball should be checked frequently, and it must be replaced if it is less than 15.675MM.

六、注意事项：

★该机采用三相380V电源，机外壳必须接地，设备未经可靠接地严禁使用。

★磨头在运转过程中，百分表必须固定，百分表测量头和顶板脱离接触，当运转停止，测量头与顶板接触并读数。

★在试验中，百分表测得磨面面深度≯1.5mm，以防磨头的轴承架磨损毁坏，不准继续试验。

★本机采用传感器接收系统测量磨头转数，一旦发现磨头在运转而控制器的数码显示停止，应立即停机，检查传感器（6）的位置是否处于传感器接收区域。

6. Matters needing attention:

★The machine adopts three-phase 380V power supply, the shell of the machine must be grounded, and the equipment is strictly prohibited to use without reliable grounding.

★During the operation of the grinding head, the dial indicator must be fixed, and the dial indicator measuring head is out of contact with the top plate. When the operation stops, the measuring head contacts the top plate and reads.

★During the test, the depth of the grinding surface measured by the dial indicator is ≯1.5mm, in order to prevent the bearing frame of the grinding head from being worn and damaged, and the test is not allowed to continue.

★This machine uses a sensor receiving system to measure the number of revolutions of the grinding head. Once it is found that the grinding head is running and the digital display of the controller stops, stop it immediately and check whether the position of the sensor (6) is in the sensor receiving area.

七、装箱单：

★耐磨试验机1台

★控制器1台

★磨头（滚珠轴承）1件

★百分表 1只

★升降手柄 1件

★锁紧手柄1件

★配重块1件

★说明书1本

★合格证1张。

7. Packing list:

★1 abrasion resistance testing machine

★ 1 controller

★ 1 piece of grinding head (ball bearing)

★ Dial indicator 1

★ Lifting handle 1 piece

★ 1 lock handle

★1 counterweight

★1 manual

★One certificate of conformity.