- Nanofocus μSurf (白光共轭焦轮廓仪)

产品类型：白光、共轭焦、非接触

μSurf结合CCD的影像摄取，以有许多孔洞的旋转盘取代侦测器的孔洞，再将物鏡垂直移动，以类似断层摄影方式，精确量测物体高度（如下图所示）。

由于使用了共轭焦的方法，在测量渐变较大的高度时，跟其他同类公司产品使用较多的干涉法相比，可以精确量测物体高度，建立3D立体影像，优势相当明显。

- 应用

μSurf用来测量表面物理形貌，如3D表面形貌、2D的纵深形貌、轮廓（纵深、宽度、曲率、角度）、表面粗糙度等。其测量方式是非接触式，不会破坏样品的表面，不需要在真空环境下测量，也可以用显微镜测量的功能来观测样本。

  - 精密部件：检测对表面磨损，表面粗糙度，表面微结构有要求的零部件，比如发动机汽缸;

  - 生命科学：测量stents支架上镀层厚度等

  - 微电子机械系统：微型器件的检测，医药工程中组织结构的检测，如基因芯片等

  - 半导体: 检测微型电子系统，封装及辅助产品结构设计

[1] micro lenses       [2] paper    [3] Lasertex sheet metal  [4] Pretex sheet metal

- 技术参数

| Measuring head | CX | CI |
| --- | --- | --- |
| Image acquistion module BM 512 | Digital camera with progressive- scan technology, up to 25fps, 512 x 512 Pixel, 8bit, Firewire | Fast digital camera with progressive- scan technology, up to 58fps, 512 x 512 Pixel, 12 Bit, Firewirs |
| light source, adjustable | Halogen light source (LS 100) | Powerfull-Xe-light source (LX 100, LX 180) |

| Scan modules |  |
| --- | --- |
| x, y-axis module MS 50 | Precision x, y-table, 50 x 50mm, resolution 0.1μm |
| z-axis module ZM 100 | Precision scanning module, range 100mm, resolution 0.1μm |
| z-axis module NV 350 | - | Fast precision scanning module (Piezo), measuring range 350μm, resolution < 1nm |

| Optic modules1) | 1600 S | 800 L / S / XS | 320 L / S / XS | 160 L / S |
| --- | --- | --- | --- | --- |
| Measurement area (x/y)(um)2 (XY测量范围) | 1600 x 1600 | 800 x 800 | 320 x 320 | 160 x 160 |
| Numerical aperture (NA值) | 0.3 | 0.4 / 0.46 / 0.6 | 0.5 / 0.8 / 0.95 | 0.8 / 0.95 |
| Working distance(mm) Z方向测量范围 | 10.1 | 12 / 3.1 / 0.9 | 10.6 / 0.66 / 0.3 | 3.4 / 0.31 |
| Resolution in z-direction(nm)CX (Z方向范围分辨率) CI2) | 50 20 | 35 / 30 / - 6 / 5 / 4 | 25 / 15 / - 4 / 2 / 2 | - 2 / 1 |
| Resolution in x,y-direction (XY分辨率) | 2.9 | 1.5 | 0.6 | 0.31 |
| 1) L : long working distance, S : normal working distance, XS : short working distance, 2) noise level (only with NV350) |